## Slide 1: Effect of hydrogen bonding on spectroscopic properties in organic-inorganic hybrids
Magdalena Wachowiak
Supervisor: dr hab. Łukasz Hetmańczyk

## Slide 2: Goals
The thermal measurements of three samples belonging do coordination polymers in order to determine the thermal stability (TGA) and to detect the solid-to-solid phase transition (DSC).
The measurement of Raman spectra for the crystals at room temperature, and the comparison with results obtained from infrared spectroscopy.
Theoretical prediction of IR and RS spectra and their comparison with experimental ones.
Some remarks on hydrogen bonds in the measured samples.
Notes: Charakterystyka spektroskopowa, termiczna, wiązania wodorowe, wiązanie metal - węgiel

## Slide 3: Hybrids of organic-inorganic perovskites (HOIPs)
[A]2B’B”(X)6
A – organic cation, acetamidinium
B’ – K+
B” – Cr3+, Fe3+, Co3+
X – CN-

## Slide 4: HOIPs

## Slide 5: Thermal Gravimetric Analysis, TGA
ACECr
Notes: Stabilna do 250 st. C

## Slide 6: Differential Scanning Calorimetry, DSC
ACECr
ACEFe
ACECo

## Slide 7: Crystal structure ACECr
low intermediate high

## Slide 8: Experimental spectra
Raman spectra:
Horriba LabRam HR Evolution
Dispersive spectrometer
Incident laser wavelength 633 nm
Power: 100% (50% Fe)
Objective: 100x
Wavelength: 50 – 3600 cm-1
Accumulation: 9s
Repetition: 6 times

## Slide 9: Experimental spectra
IR spectra:
Bruker Vertex 70v
Fourier transform, vacuum
MIR
  range: 400 – 4000 cm-1
  sample suspended in nujol, put on KBr pellet
  32 scans
  KBr beamsplitter
FIR
  range: 30 – 600 cm-1
  sample suspended in apiezon, put on PE disc
  32 scans
  Si beamsplitter

## Slide 10: Optical spectra calculation
What for?
To support interpretation of experimental spectra.
The best way: calculation for crystal (solid state) using Periodic Boundary Conditions → phonons.
But …
The systems under investigation are dynamically disordered (even at low temperatures)
Calculations are time consuming → we were time limited.
The spectra were calculated as a sum of constituting molecules:
→ MIR spectra (internal vibrations) are reasonably well reproduced (despite the simplicity of the assumed model),
→ FIR (especially low wavenumber region); lattice vibrations are missing.

## Slide 11: IR and RS spectroscopy
Method: DFT
Functional: Genaral Ggradient Approximation, PBE + D3BJ dispersion correction (Grimme)
Basis set: TZVPP
Program: ORCA v. 4.1.1
+
Building blocks
All complexes in the CN- octahedral field
are low spin states:
Cr3+ = [Ar]3d3 (2S+1 = 4)
Fe3+ = [Ar]3d5 (2S+1 = 2)
Co3+ = [Ar]3d6 (2S+1 = 1)
Symmetry: Oh (48 symmetry elements)
Γvib: 2A1g + 2Eg + T1g + 2T2g + 4T1u + 2T2u
IR active: 4T1u
RS active: 2A1g + 2Eg + 2T2g
Symmetry: Cs (only one plane)
Γvib: 15A’ + 12A”
IR active: 15A’ + 12A”
RS active: 15A’ + 12A”
Notes: The total spectrum was approximated by a sum of spectra calculated for particular isolated molecules

## Slide 12: Spectroscopic analysis- ACECo
C-N
Notes: Raman, IR

## Slide 13: ACEFe
Notes: Drgania w ramanie i IR

## Slide 14: ACECr

## Slide 15: Hydrogen bond
~2.5 Å
~3.5 Å
angle N-H…N = 150°

## Slide 16: Hydrogen bonding
Notes: Drgania 2X: symetryczne nie w fazie, asymetryczne

## Slide 17: Conclusions
The investigated compounds have two solid-solid phase transitions in the temperature range from -150°C to 150°C.
The samples are thermally stable up to ~220°C.
The calculated IR and RS spectra are in a good agreement with experimental.
Hydrogen bonds are rather weak and are of similar strength in discussed complex. In high temperature phases the organic cation is strongly dynamically disordered.

## Slide 18
Thank you…..